## Slide 1: Transient Simulation of Detrap Failure under Retention Operation of BETOX 3D NAND Flash Cell 진명

## Slide 2: Research Flow
0.6 eV Elastic
0.8 eV Elastic
1.5 eV Elastic
μ = 0.85 [eV], σ = 0.25 [eV]
Gaussian distribution trap profile fit
Single level trap profile fit
①
②
TBT Emission model
Simulation time reduction

## Slide 3: Previous Studies
김민수 박사 Detrap 논문 내용
Single level trap profile
Poole-Frenkel Emission
Non-linear differential equation
term makes nonlinearity

## Slide 4: Freezing CTN (TCAD Know-how)
By minimizing capture cross section
(⸪ Poole-Frenkel emission ~ σn )
: Result of CTN LM turn-on/off
σn : 10-15 [cm2] → 10-30 [cm2]

## Slide 5: Simplifying the Detrap Model
Thermal emission negligible
Large time constant
High Vertical Electrical Field
BETOX Nitride Region
Vertical direct tunneling negligible
Rather than direct tunneling,
lateral directional spreading may occur
Result…
Only TBT is left
…

## Slide 6: Tunneling through Trapezoidal Barrier (TC)
①
②
①
②
: WKB approximation under uniform field trapezodidal barrier
Double Barrier Emission: Simple Multiplication ( TCtotal = ① x ② )
ΦH, ΦL, Feq dependent

## Slide 7: Tunneling through Trapezoidal Barrier (TC)
Uniform Field Assumption
ox1 layer
n1 layer
ox2 layer
CTN
BE-TOX (ONO)
Electric Field
Low field intensity difference (< 8%) … reference field set to centroid

## Slide 8: Trap-to-Band Tunneling Current Modeling (νTBT)
Region 1
(reservoir)
Region 2
SRH
Statistics
Trap-interface coupling
Tunneling
Capture-Emission
Statistics
EF,r
EC,r
EV,r
EC
EV
Etrap
Trap-interface coupling
Region 1 as carrier reservoir
  Fermi statistics follows Region 1: EF,r
Tunneling capture-emission statistics
Follows “Principle of Detailed Balance”

## Slide 9: Trap-to-Band Tunneling Current Modeling (νTBT)
Principle of Detailed Balance
Similar to SRH recombination-generation theory,
Emission of electron/hole is in steady state coupled to tunneling from carrier reservoir
(in this case, carrier reservoir is CB of channel)
ox1 layer
n1 layer
ox2 layer
CTN
BE-TOX (ONO)

## Slide 10: Trap-to-Band Tunneling Current Modeling (νTBT)
: Transition rate by Fermi golden rule
: Constant perturbation of energy band by trap
: Unperturbed energy band free electron
: Trapped electron
Constant Trap
Free wave eq.

## Slide 11: Trap-to-Band Tunneling Current Modeling (νTBT)

## Slide 12: Trap-to-Band Tunneling Current Modeling (νTBT)
(at Et = 0.8eV single level)
Additional information
VT = 10-33 [m3] = (0.1Å)3 = (λe)3 : ideally trapped electron (λe : electron matter wavelength)
Etrap : Energy level of trapped electron
|ET| : Energy level difference from conduction band
~0.1Å
(reservoir)
EF,r
EC,r
EV,r
EC
EV
Etrap
|ET|
Etrap – EC,r

## Slide 13: Simulation Method
ox1 layer
n1 layer
ox2 layer
CTN
BE-TOX (ONO)
BE-TOX
“Centered balance point”
λ used as a fitting parameter
(0< λ<1)
Fn, j
Fox
(rtox,center)
coordinate
Energy Band
λ
1-λ
ΦH
ΦL
eTBT, j
(for all j segments)
TCj
… eTBT, j = νTBT x TCj

## Slide 14: Simulation Method
…
More segments,
More precise result
n segments

## Slide 15: Final Result of Retention Transient
Gaussian distribution trap profile fit
Single level trap profile fit
Can be adopted to various
trap profile & PV levels!

## Slide 16: Simulation Time Reduction
Chart: 
| TCAD | ODE Simulation | General Solution Simulation
계열 1 | 4 | 2 | 0.2
열1
열2
~ 20,000-40,000 s
~ 10-30 s
~ 0.02 s
Simulation Time Reduction
General Solution
Simulation
→ no ODE Solving
ODE Simulation
→ operation oriented
Time Reduction