## Slide 1: Autonomous Physics-Based Modeling of Retention Loss in 3-D NAND Flash Memory in Cryogenic condition EDL Manuscript Change & Progress Myung Jin

## Slide 2: Detailed Poisson Solution
Fig. 1
(b) pgm charge
Charge distribution model adapted
최해찬/유진일 TED 2024
이찬 JJAP 2026
JJAP 65 (2026) 011004
IEEE T-ED 71 (2024) 2386–2392

## Slide 3: Cryogenic and Detrapping
Measurement (Refaldi, IRPS 2025)
Cryogenic condition (~ 4.2K) : physical separation of detrapping effect
Separation of detrapping effect measurement
**Time is in not in A.U. : calibration of time constant can be done

## Slide 4: Cryogenic and Detrapping
Deactivate Conduction band – trap interaction
Cryogenic
Measurement calibration result:
Used scale
O/N/O = 3/6/8 [nm]
(cf. DRL spec: 5/6/8 [nm])

## Slide 5: Autonomous Modeling & Result
TCAD – model Matching
TOX variation
3/3.5/4/4.5/5 [nm]
Well match with TCAD - model

## Slide 6: Progress with paper
Done progress
Measurement calibration figure added
TCAD-model matching figure added
On-going progress
Benchmark information
Referencing