## Slide 1: (EDL manuscript) Time-step-free Physics-Based Modeling of Retention Loss in Cryogenic 3-D NAND Flash 연구 요약 진명

## Slide 2: Detailed Poisson Solution / Q-ΔVth Relation
Potential Solution: Poisson equation
Boundary conditions
Solution
Q-ΔVth Relation
>> computation optimization
ΔVth calculation can be done with
single determinant

## Slide 3: Visualization & Parameters

## Slide 4: Time-step-free Physics-based Modeling
1. Initial state
nt0(r, Et)
2. Emission rates
ech, eWL
3. Direct evaluation
nt(r, Et, t)
Emission evaluation
Jin, IEEE TED (2025)
Initial state definition

## Slide 5: Cryogenic Calibration
Measurement (Refaldi, IRPS 2025)
tTOX
= 3, 3.5, 4, 4.5, 5 [nm]
Measurement – TCAD calibration
TCAD cryogenic: σ → 0 cm2
O/N/O = 3/6/8
model – TCAD match
tTOX = 3 ~ 5 [nm]

## Slide 6: Computational Impact
Property
Transient TCAD
Time-step-free model
Temporal
treatment
Sequential
time stepping
Final-time
dependence
Runtime grows as
simulated retention time increases
Independent of final
physical time for fixed queries
Average
runtime
27483 s
3.926 s
Closed-form
evaluation of Eq. (13)
≈ 7000×
runtime reduction
TCAD 는 final physical time까지 time step 별 순차적으로 계산
Time-step-free model은 closed-form evaluation
Computational resource는 final retention time 자체가 아니라 trap bin 수와 evaluated time point 수에 의해 결정