## Slide 1
School of Electrical Engineering, Seoul National University
1/8
Modeling of Attempt-to-Escape Frequency under Detrap Retention of Bandgap-Enginnered 3D NAND Flash Memory Cell
진명

## Slide 2
School of Electrical Engineering, Seoul National University
2/8
Direct Tunneling current Modeling : Elastic Tunneling
, same for y, z
…
Attempt-to-Escape Frequency : Elastic Tunneling
Shiely, James Patrick. Simulation of tunneling in MOS devices. Duke University, 1999.

## Slide 3
School of Electrical Engineering, Seoul National University
Attempt-to-Escape Frequency : Elastic Tunneling
3/8
Result :
* Crucial Assumption
Electron in conduction band exists only within δE.
Quasi-Fermi level is formed at the tunneling barrier
TC(EB)
No electron region
ν can be changed by the device scale

## Slide 4
School of Electrical Engineering, Seoul National University
Elastic Tunneling Modeling
4/8
Direct Tunneling
Trap to Band Tunneling
Assumption :
(Surface)Current : TOX1 – BENitride interface region area
TOX2
BENitride
TOX1
Filler + channel
TOX1-BENitride interface
Retention Current
TOX1-BENitride interface

## Slide 5
School of Electrical Engineering, Seoul National University
Remind) 24.4 Detrap TCAD Calibration
5/8
TCAD Calibration result from 24.4 >> νDT = 550 : consistent with the modeling
Fitting with α’DT
is valid enough

## Slide 6
School of Electrical Engineering, Seoul National University
TCAD Detrap Simulation Method
6/8
eXsection, hXsection 1e-15~1e-16 => 1e-30 축소를 통한 ctn emission off
∵ νPF = NCvthσc => σc의 변수 직접 조정으로 ctn의 trapped electron lock
σc,e = 2x10-15 , σc,h = 1x10-15 [cm-2]
σc,e = 2x10-30 , σc,h = 1x10-30 [cm-2]
256s Retention
256s Retention
LM occured
No LM
256s Retention

## Slide 7
School of Electrical Engineering, Seoul National University
TCAD Detrap Simulation Method
7/8
Chart: LM vs noLM by e/hXsection Control
| 9.9999999999999995E-8 | 9.9999999999999995E-7 | 1.0000000000000001E-5 | 1E-4 | 1E-3 | 0.01 | 0.1 | 0.2 | 0.5 | 1 | 2 | 4 | 8 | 16 | 32 | 64 | 128 | 256
LM | 0 | 0.00076159 | 0.0043834 | 0.014587 | 0.033607 | 0.060577 | 0.08157 | 0.086099 | 0.091618 | 0.095194 | 0.098696 | 0.10235 | 0.10631 | 0.11063 | 0.11523 | 0.11992 | 0.12456 | 0.12899
noLM | 0 | 0.00046906 | 0.0044675 | 0.020582 | 0.04238 | 0.055423 | 0.05831 | 0.058378 | 0.058401 | 0.058403 | 0.058404 | 0.058404 | 0.058404 | 0.058404 | 0.058404 | 0.058404 | 0.058407 | 0.058404
σc,e = 2x10-15 , σc,h = 1x10-15 [cm-2]
σc,e = 2x10-30 , σc,h = 1x10-30 [cm-2]
Capture Cross Section 조절을 통하여 CTN 영역의 전자의 움직임을 최소화 할 수 있음.

## Slide 8
School of Electrical Engineering, Seoul National University
Future Works
8/8
TCAD Calibration
Device spec : DRL BE-TOX 가장 최신 spec 활용 예정
Trap profile : discrete level 활용 예정 (ex. 0.5eV, 0.6eV…)
3D Modified Poole-Frenkel Emission
α’ Calibration